## Slide 1: Mechanistic Study of intermediates in the water oxidation pathway
By: Seth Croslow
Mentor: Chaochao Lang
PI: Dr. Dunwei Wang

## Slide 2: Project Overview
Sample
Two proposed O-O bond formation mechanisms:
IMOC:
WHAA:
Water Oxidation
Cobalt Catalyst
O-O Bond Forming Intermediates
Methods
Fourier Transform Infrared Spectroscopy
Electrochemical Tests
J. Am. Chem. Soc. 2016, 138, 4229−4236

## Slide 3: Oxygen Evolution Reaction Pathway
J. Am. Chem. Soc. 2016, 138, 4229−4236
Two proposed O-O bond formation mechanisms:
IMOC:
WHAA:
O-O bond formation, rds
PCET
pre-equilibrium

## Slide 4: Steady state Tafel – Water-In-Salt
Salt-in-Water
Science, 2015, 6263, 938-943
IMOC:
Low Potential
WHAA:
High Potential

## Slide 5: Fourier Transform Infrared Spectroscopy
Sample
Peroxide:
Superoxide:
Nat. Chem., 2014, 6, 362-367
1013 cm-1
740-920 cm-1

## Slide 6: FTIR Configurations
Catalyst deposited directly onto crystal
Small background interference
FTO working electrode with catalyst placed onto crystal
Large background interference
Otto Configuration:
mutil-bounce ZnSe ATR crystal
Kretschmann Configuration:
micro-machined Si ATR wafer
F
ZnSe
WE
Si
WE

## Slide 7
H2O
D2O
H218O
H2O vs. D2O vs. H218O
1,014 peak: potential reversible
820 peak: not potential reversible
  Maybe not an intermediate
1,014 peak: no shift
  No H in intermediate
820 peak: constant/unchanged
1,014 peak: shifted to 966
  Indication of 18O—18O bond

## Slide 8
D2O Confirmation/Comparison
Distinct peak in 0.1 M KCl D2O
  Removes the 987 cm-1 phosphate band
  Confirms the validity of the 1014 cm-1 peak
  Test isotope effect
    H2O
    D2O
    H218O

## Slide 9: Water-In-Salt - FTIR

## Slide 10: Summary
Steady state measurements:
  Increased dependence on water as potential increased
  Mechanism switch from IMOC to WHAA?
FTIR data:
  Co-O-O-Co intermediate at high potentials
  No presence of the Co-O-OH intermediate
  Possible decrease in Co-O-O-Co peak in reduced water activity
FTIR data does not currently prove or disprove the mechanism switch hypothesis
Notes: The two intermediates could be present simultaneously, but only see the one peak. In rebuttal to increase of peak intensity with increasing potential: as the potential increases, the rate also increases, so it could be that the rate of the superoxide intermediate just increases at a faster rate.

## Slide 11: Future Plans
Electrochemical Quartz Crystal Microbalance
  Quantify water adsorption on catalyst during steady state
FTIR
  Perform additional water-in-salt experiments
  Try to reduce the effect of phosphate bands

## Slide 12: Acknowledgements
Chaochao Lang
Jingyi Li
Dr. Dunwei Wang
Boston College REU Program

## Slide 13: Questions
Thank You!
Project Overview
Oxygen Evolution Reaction Pathway
Steady state Tafel – Water-In-Salt
Fourier Transform Infrared Spectroscopy
FTIR Configurations
H2O vs. D2O vs. H218O
D20 Confirmation/Comparison
Summary

## Slide 14: Electrochemical Quartz Crystal Microbalance
Inverse Piezoelectric Effect:
  Upon application of a potential difference to the crystal, acoustic sound waves are produced
  A change in mass results in a change in the fundamental frequency
Sauerbrey Equation:
  where:
    m = change in mass
    C = 17.7 ngHz-1cm-2
    f = change in resonant frequency
    n = 1, 3, 5, … is the overtone number

## Slide 15: CoOx Film Deposition
Utilizes two electrode system:
  Working Electrode
  Counter Electrode
Method:
  Solutions:
    0.01 M Co(NO3)2
    0.1 M NaCH3CO2
  Galvanostatic
    Constant current: 0.05 mA
    Duration: 322 s
Catalyst is used to facilitate oxygen evolution

## Slide 16: H2O vs. D2O vs. H218O
H2O
D2O
H218O

## Slide 17: Summary
Steady state measurements:
  Increased dependence on water as potential increased
  Mechanism switch from IMOC to WHAA?
FTIR peak at ~1014 cm-1:
  Shifted to ~966 cm-1 in H218O with no shift in D2O
  Peak is most likely Co-O-O-Co intermediate
FTIR peak at ~820:
  Showed no potential reversibility in H2O and no similar peaks in D2O or H218O
  No confirmation of the Co-O-OH intermediate
FTIR data does not prove or disprove the mechanism switch hypothesis

## Slide 18
D20 Confirmation/comparison
Distinct peak in 0.1 M KCl D2O
  Removes the 987 cm-1 phosphate peak
  Confirms the validity of the 1014 cm-1 peak
Catalyst stability in 0.1 M KCl D2O was worse
  Test isotope effect
    H2O
    D2O
    H218O
0.1 M KCl D2O
0.1 M KPi D2O
Notes: Maybe just delete the CV comparison???

## Slide 19: Fourier Transform Infrared Spectroscopy
Background:
  IR radiation is passed through sample which absorbs some of the light at specific frequencies
  Absorption is determined by:
    Mass of atoms
    Strength of bond
  Frequency shift due to isotopic effect can be calculated using the following equation:
Sample

## Slide 20: Motivation
Current Usage: 154,000 TWh/year
Expected Growth by 2040: 28% increase
  43,000 TWh/year
  17.2 Billion tons of coal
  8,600 new nuclear power plants
Water oxidation could be the key to solving this energy crisis
  Use sunlight to produce O2 and H2
  Burn O2 and H2 to get energy and water

## Slide 21: Water-In-Salt - FTIR
7 M NaNO3
0 M NaNO3